ARP ANTHONY RICHARDSON AND PARTNERS
3023/01
SURVEY REPORT AT DEREGISTRATION
20.01.09
	PROPERTY: 
	1-50 Wesley Square, London W11
AREA: 1.2 Hectares

	
	

	CLIENT:
	Maunsel Fourth Coownership Housing Society Ltd

	
	

	DESCRIPTION:
	3 Terraces built around a garden following the square constructed in 1978
(see attached site plan 3023H)

	
	

	CURTILAGES:  
	Front: (to the garden)
Rear: (to perimeter roads)

	
	6.75 x average 6.0m
6.75 x AV 8.0m

	SUB-STRUCTURE
	
	

	Founds and u/p/g:
	Concrete strip footings.
	Good condition no visible movements.

	DPC:
	Felt roll bitumen DPC.
	Good, no defects visible.

	Ground Floor:
	Concrete slab, reinforced 225 deep.
	Good, no visible defects.

	ROOF:
	
	

	Structure:
	150 x 150 SW joists and purlins.
	Terrace 25-30 has deflections on west slope.  Other are in good condition.

	Coverings:
	Marley ‘Modern’ concrete interlocking tiles on felt underlay.
	Uneven tiles around rooflights and vents in places but generally good condition.

	Stacks/parapets:
	No stacks/parapets PVC vents
	Ridges loose.  Vent stack flashings are uneven and weak.

	Rainwater goods:
	Plastic black PVC.
	Old, requires replacement.

	STRUCTURE:
	
	

	External Walls:
	Brick facings with cavity and inner skin of 100mm dense block no insulation.
	All in good condition.

Cavity is blocked in places.

	Windows & Ex Doors:
	Timber, EDJMA sections

Some double glazed
	All repaired 2007.  Good condition.  Some repairs required in 2012 redecs.

	Upper Floors:
	Timber joists 150 x 50 SW
	All good condition.

	Int Walls & Partitions:
	75mm block on GF.

Stud and plasterboard on upper floors.
	All in good condition.

	Int Doors & Joinery:
	Timber flush doors

Various joinery
	Good condition.


	FINISHES:
	
	

	Walls and ceilings:
	Plaster, generally papered – various.
	Good condition.

	DECORATIONS:
	
	

	Internal:
	Various residents decorations.
	All in good condition.

	External:
	Painted wood.  Sikkens repainted in 2007.
	Good condition.

	FITTINGS:
	
	

	Kitchen:
	Residents fittings.
	-

	Bathroom:
	Residents fittings
	-

	PLUMBING AND WASTES:
	Residents fittings
	-

	HEATING:
	Residents installation
	-

	ELECTRICAL:
	Common area and external lights repaired and replaced 2006.
	-

	SERVICE CONNECTIONS:
	Gas
Water

Electricity
	

	INSULATION:
	None
	

	INFESTATION:

(TREATMENT)
	Timber work checked 2008.
	No visible defects.

	DRAINS:
	Unaltered as built drains in salt glazed clay.
	

	EXTERNAL WORKS:
	Paving to paths conc 600sq
Fences in timber repaired 2006
	Paving in poor condition.
Gates and fences in good condition.

	SUNDRIES:
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